GL-A500 STEEL PLATE

Gangsteel is specialized in supplying GL extra high strength steel plate in GL Grade A500. For more information of Grade A500 steel plate, please check them in following:

| GL-A500 extra High Strength Chemical Composition Tempering and Quenching |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade | The Element Max (%) |  |  |  |  |  |  |
|  | C | Si | Mn | P | S | Al(min) | N |
| GL-A500 | 0.21 | 0.55 | 1.70 | 0.035 | 0.035 | 0.015 | 0.020 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| GL-A500 extra High strength property in Tempering and Quenching |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Grade | Mechanical Property |  |  | Charpy V Impact Test |  |  |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| GL-A500 | Min Mpa | Mpa | Min % | 0 | J | J |
|  | 500 | 610-770 | 16% |  | 33 | 50 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |  |  |  |  |  |  |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of GL-A500 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV A500 | GL-A500 | LR/AH50 | BV/A500 | CCS/A500 | K A51 | R A51 | RI/A500 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.