GL-A40 STEEL PLATE

Gangsteel is specialized in supplying GL high strength steel plate in GL Grade AH40. For more information of Grade AH40 steel plate, please check them in following:

| GL-A40 high Strength Chemical Composition in Tempering and Quenching |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade | The Element Max (%) |  |  |  |  |  |  |
|  | C | Si | Mn | P | S | Al | N |
| GL-A40 | 0.18 | 0.50 | 0.90-1.6 | 0.035 | 0.035 | 0.015 |  |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.05-0.10 | 0.02 | 0.30 | 0.2 | 0.4 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| GL-A40 high strength property in tempering and quenching |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade |  | Mechanical Property |  |  | Charpy V Impact Test |  |  |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| GL-A40 | mm | Min Mpa | Mpa | Min % | 0 | J | J |
|  | t≤50 | 390 | 510-660 | 20% |  | 27 | 41 |
|  | 50＜t≤70 | 390 | 510-660 | 20% |  | 31 | 46 |
|  | 70＜t≤100 | 390 | 510-660 | 20% |  | 37 | 55 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |  |  |  |  |  |  |  |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of GL-A40 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV A40 | GL-A40 | LR/AH40 | BV/AH40 | CCS/A40 | K A40 | R A40 | RI/A40 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.