NK GRADE KA STEEL PLATE

Gangsteel is specialized in supplying NK extra strength steel plate in NK Grade K A. For more information of Grade K A steel plate, please check them in following:

| NK GRADE KA general Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al |
| NK GRADE KA | 0.21 | 0.50 | 2.5*C | 0.035 | 0.035 | 0.015 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| NK GRADE KA general strength property |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | -- | 27 | 20 |
| NK GRADE KA | 235 | 400-520 | 22 |  |  |  |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of NK GRADE KA |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV K A | GL K A | LR/K A | BV/K A | CCS/K A | K A | R A | RI/K A |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes