NK/K B STEEL PLATE

Gangsteel is specialized in supplying NK extra strength steel plate in NK Grade K B. For more information of Grade K B steel plate, please check them in following:

| NK/K B general Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al |
| NK/K B | 0.21 | 0.50 | 2.5*C | 0.035 | 0.035 | - |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| NK/K B general strength property |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | 0 | 27 | 20 |
| NK/K B | 235 | 400-520 | 22 |  |  |  |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of NK/K B |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV K B | GL K B | LR/K B | BV/K B | CCS/K B | K B | R B | RI/K B |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes