NK/K A47 STEEL PLATE

Gangsteel is specialized in supplying NK extra strength steel plate in NK Grade K A47. For more information of Grade K A47 steel plate, please check them in following:

| NK/K A47 extra Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al | N |
| NK/K A47 | 0.21 | 0.55 | 1.70 | 0.030 | 0.030 | - | 0.020 |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | - | - | - | - | - | - | - |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| NK/K A47 extra strength property |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | 0 | 46 | 31 |
| NK/K A47 | 460 | 570-720 | 17 |  |  |  |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of NK/K A47 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV A47 | GL A47 | LR/A47 | BV/A47 | CCS/A47 | K A47 | R A47 | RI A47 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes