NK/K D36 STEEL PLATE

Gangsteel is specialized in supplying NK extra strength steel plate in NK Grade K D36. For more information of Grade K D36 steel plate, please check them in following:

| NK/K D36 high Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al | N |
| NK/K D36 | 0.18 | 0.50 | 0.90-1.6 | 0.035 | 0.035 | 0.015 |  |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.05-0.10 | 0.02 | 0.35 | 0.2 | 0.4 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| NK/K D36 high strength property |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | -20 | 34 | 24 |
| NK/K D36 | 355 | 490-620 | 21 |  |  |  |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of NK/K D36 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV D36 | GL D36 | LR/D36 | BV/D36 | CCS/D36 | K D36 | R D36 | RI D36 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes