- S275NL| S275NL steel plate

| Gangsteel Grade : | S275NL(1.0491) |
| --- | --- |
| Specification: | Thickness 8mm-300mm, Width: 1500-4020mm, Length: 3000-27000mm |
| Standard: | EN 10025 - 3 : 2004 Technical delivery conditions for normalized/normalized rolled weldable fine grain structural steels |
| Approval By Third Party | ABS, DNV, GL, CCS, LR , RINA, KR, TUV, CE |
| Classification: | Normalized rolled weldable fine grain structural steels |

Gangsteel is specialized in supplying EN10025-3 steel plate in S275NL. For more information of S275NL steel plates, please check them in following:

Chemical composition % of the Product analysis of grade S275NL (1.0491)

Nominal thickness =< 63(mm) CEV max = 0.4
Nominal thickness from 63 to 100 (mm) CEV max = 0. 4

Nominal thickness from 100 to 250 (mm) CEV max = 0. 42

| C | Si | Mn | Ni | P | S | Cr | Mo |
| --- | --- | --- | --- | --- | --- | --- | --- |
| max 0.16 | max 0.45 | 0,45 -1,60 | max 0.35 | max 0.3 | max0.025 | max 0.35 | max 0.13 |
| V | Nb | Ti |  |  |  |  |  |
| max 0.07 | max 0.06 | max 0.06 |  |  |  |  |  |

Mechanical properties of grade   S275NL (1.0491)

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |

| Nominal thickness (mm) | to 16 | 16 - 40 | 40 - 63 | 63 - 80 | 80 - 100 | 100 - 150 | 150 - 200 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ReH - Minimum yield strength (MPa) | 275 | 265 | 255 | 245 | 235 | 225 | 215 |

| Nominal thickness (mm) | to 100 | 100 - 200 |
| --- | --- | --- |
| Rm -Tensile strength (MPa) | 370-510 | 350-480 |

| Nominal thickness (mm) | to 16 | 16 - 40 | 40 - 63 | 63 - 80 | 80 - 200 |
| --- | --- | --- | --- | --- | --- |
| A - Minimum elongation Lo = 5,65 √ So (%) | 24 | 24 | 24 | 23 | 23. |

Equivalent grades of grade S275NL (1.0491)

| Germany DIN,WNr | France AFNOR | England BS | Italy UNI | China GB | Russia GOST |
| --- | --- | --- | --- | --- | --- |
| TStE285 |  | 43EE | Fe E 275 KT N |  |  |

Related grades: S355N|S420N|S420NL|S460N|S460NL