- EN10025-3 S420NL| S420NL steel plate

| Gangsteel Grade : | S420NL(1.8912) |
| --- | --- |
| Specification: | Thickness 8mm-300mm, Width: 1500-4020mm, Length: 3000-27000mm |
| Standard: | EN 10025 - 3:2004 Technical delivery conditions for normalized/normalized rolled weldable fine grain structural steels |
| Approval By Third Party | ABS, DNV, GL, CCS, LR , RINA, KR, TUV, CE |
| Classification: | Normalized rolled weldable fine grain structural steels |

Gangsteel is specialized in supplying EN10025-3 steel plate in S420NL. For more information of S420NL steel plates, please check them in following:

Chemical composition % of the Product analysis of grade S420NL (1.8912)

Nominal thickness =< 63(mm) CEV max = 0.48
Nominal thickness from 63 to 100 (mm) CEV max = 0.50

| C | Si | Mn | Ni | P | S | Cr | Mo |
| --- | --- | --- | --- | --- | --- | --- | --- |
| max 0.2 | max 0.6 | 1-1.7 | max 0.8 | max 0.025 | max 0.020 | max 0.3 | max 0.1 |
| V | Nb | Ti |  |  |  |  |  |
| max 0.2 | max 0.05 | max 0.05 |  |  |  |  |  |

Mechanical properties of grade   S420NL (1.8912)

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |

| Nominal thickness (mm) | to 16 | 16 - 40 | 40 - 63 | 63 - 80 | 80 - 100 | 100 - 150 | 150 - 200 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ReH - Minimum yield strength (MPa) | 420 | 400 | 390 | 370 | 360 | 340 | 330 |

| Nominal thickness (mm) | to 100 | 100 - 200 |
| --- | --- | --- |
| Rm -Tensile strength (MPa) | 520-680 | 500-650 |

| Nominal thickness (mm) | to 16 | 16 - 40 | 40 - 63 | 63 - 80 | 80 - 200 |
| --- | --- | --- | --- | --- | --- |
| A - Minimum elongation Lo = 5,65 √ So (%) | 19 | 19 | 19 | 18 | 18. |

Equivalent grades of grade S420NL (1.8912)

| Germany DIN,WNr | France AFNOR | England BS | Italy UNI | China GB | Russia GOST |
| --- | --- | --- | --- | --- | --- |
| TStE420 | E 420 FP |  |  |  |  |

Related grades: S355N|S420N|S355NL|S460N|S460NL