- EN10025-3 S460N| S460N steel plate

| Gangsteel Grade : | S460N(1.8901) |
| --- | --- |
| Specification: | Thickness 8mm-300mm, Width: 1500-4020mm, Length: 3000-27000mm |
| Standard: | EN 10025 - 3:2004 Technical delivery conditions for normalized/normalized rolled weldable fine grain structural steels |
| Approval By Third Party | ABS, DNV, GL, CCS, LR , RINA, KR, TUV, CE |
| Classification: | Normalized rolled weldable fine grain structural steels |

Gangsteel is specialized in supplying EN10025-3 steel plate in S460N. For more information of S460N steel plates, please check them in following:

Chemical composition % of the Product analysis of grade S460N (1.8901)

Nominal thickness =< 63(mm) CEV max = 0.53
Nominal thickness from 63 to 100 (mm) CEV max = 0.54

| C | Si | Mn | Ni | P | S | Cr | Mo |
| --- | --- | --- | --- | --- | --- | --- | --- |
| max 0.22 | max 0.65 | 0.95 - 1.8 | max 0.85 | ma 0.035 | max 0.03 | max 0.35 | max 0.13 |
| V | Nb | Ti |  |  |  |  |  |
| max 0.22 | max 0.06 | max 0.06 |  |  |  |  |  |

Mechanical properties of grade   S460N (1.8901)

| Temperature | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 40 | 43 | 47 | 55 |

| Nominal thickness (mm) | to 16 | 16 - 40 | 40 - 63 | 63 - 80 | 80 - 100 | 100 - 150 | 150 - 200 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ReH - Minimum yield strength (MPa) | 460 | 440 | 430 | 410 | 400 | 380 | 370 |

| Nominal thickness (mm) | to 100 | 100 - 200 |
| --- | --- | --- |
| Rm -Tensile strength (MPa) | 540 to 720 | 530 to 710 |

| Nominal thickness (mm) | to 16 | 16 - 40 | 40 - 63 | 63 - 80 | 80 - 200 |
| --- | --- | --- | --- | --- | --- |
| A - Minimum elongation Lo = 5,65 √ So (%) | 17 | 17 | 17 | 17 | 17 |

Equivalent grades of grade S460N (1.8901)

| Germany DIN,WNr | France AFNOR | England BS | Italy UNI | China GB | Russia GOST |
| --- | --- | --- | --- | --- | --- |
| StE460 | E 460 R |  | Fe E 460 KG N |  |  |

Related grades: S355N|S420NL|S355NL|S460N|S420N