A131 EH36 STEEL PLATE

Gangsteel is specialized in supplying A131 high strength steel plate in A131 Grade DH32. For more information of Grade EH36 steel plate, please check them in following:

| A131 EH36 high Strength Chemical Composition |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade | The Element Max (%) |  |  |  |  |  |  |
|  | C | Si | Mn | P | S | Al | N |
| A131 EH36 | 0.18 | 0.1-0.50 | 0.90-1.6 | 0.035 | 0.035 | 0.015 |  |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.05-0.10 | 0.02 | 0.35 | 0.2 | 0.4 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| A131 EH36 high strength property |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade |  | Mechanical Property |  |  | Charpy V Impact Test |  |  |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| A131 EH36 | mm | Min Mpa | Mpa | Min % | -40 | J | J |
|  | t≤50 | 360 | 490-620 | 19% |  | 17 | 25 |
|  | 50＜t≤70 | 360 | 490-620 | 19% |  | 19 | 28 |
|  | 70＜t≤100 | 360 | 490-620 | 19% |  | 23 | 34 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |  |  |  |  |  |  |  |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of A131 EH36 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV E36 | GL-E36 | LR/EH36 | BV/EH36 | CCS/E36 | K E36 | R E36 | RI/E36 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.