A131 FH40 STEEL PLATE

Gangsteel is specialized in supplying A131 high strength steel plate in A131 Grade FH40. For more information of GradeFH40 steel plate, please check them in following:

| A131 FH40 high Strength Chemical Composition |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade | The Element Max (%) |  |  |  |  |  |  |
|  | C | Si | Mn | P | S | Al | N |
| A131 FH40 | 0.16 | 0.1-0.50 | 0.90-1.6 | 0.025 | 0.025 | 0.015 | 0.009 |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.05-0.10 | 0.02 | 0.35 | 0.2 | 0.4 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| A131 FH40 high strength property |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade |  | Mechanical Property |  |  | Charpy V Impact Test |  |  |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| A131 FH40 | mm | Min Mpa | Mpa | Min % | -60 | J | J |
|  | t≤50 | 390 | 510-650 | 22% |  | 20 | 30 |
|  | 50＜t≤70 | 390 | 510-650 | 22% |  | - | - |
|  | 70＜t≤100 | 390 | 510-650 | 22% |  | - | - |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |  |  |  |  |  |  |  |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of A131 FH40 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV F40 | GL-F40 | LR/FH40 | BV/FH40 | CCS/F40 | K F40 | R F40 | RI/F40 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.