A131 GRADE E STEEL PLATE

Gangsteel is specialized in supplying A131 general strength steel plate in A131 Grade E For more information of Grade E Steel plate, please check them in following:

| A131 GRADE E general Strength Chemical Composition |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Grade | The Element Max (%) |  |  |  |  |  |
|  | C | Si | Mn | P | S | C+Mn/6 |
| A131 GRADE E | 0.21 | 0.10-0.35 | 0.70 | 0.035 | 0.035 | 0.40 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| A131 GRADE E high strength property |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade |  | Mechanical Property |  |  | Charpy V Impact Test |  |  |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| A131 GRADE E | mm | Min Mpa | Mpa | Min % | -40 | J | J |
|  | t≤50 | 235 | 400-520 | 21% |  | 14 | 20 |
|  | 50＜t≤70 | 235 | 400-520 | 21% |  | 17 | 25 |
|  | 70＜t≤100 | 235 | 400-520 | 21% |  | 20 | 30 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |  |  |  |  |  |  |  |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of A131 GRADE E |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV D | GL-D | LR/D | BV/D | CCS/D | K D | R D | RI/D |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.