P355N MR0175,P355N Steel plate,P355N HIC,P355N NACE

Gangsteel Bolier Plate Factory are specialized in producing and exporting EN10028-3 P355N NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

P355N,EN10028-3 P355N,P355N Steel Plate,P355N HIC,P355N Nace

Tags: P355N,EN10028-3 P355N,P355N Steel Plate,P355N steel factory, P355N adopt standard, P355N Heat treatment, P355N Technical delivery condition, P355N Chemical, P355N Mechanical property, P355N Price, P355N CEV, P355N Impact degree, P355N impact energy, P355N Supplier,P355N Specification, P355N properties, Material P355N N, P355N Material, EN10028-3 P355N, P355N Steel, P355N Yield, P355N plate, P355N HIC, P355N NACE MR0175, P355N ISO 15156, P355N NACE MR0103, P355N SSC

Keyword: P355N,EN10028-3 P355N,P355N Steel,P355N HIC, P355N NACE

- P355N Adopt standard: EN10028-3 Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- P355N Specification:  Thickness: 1mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for P355N: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- P355N Chemical composition % of the Product analysis of grade

| P355N Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al(min) | N |
| P355N | 0.20 | 0.50 | 0.9-1.70 | 0.03 | 0.025 |  | 0.02 |
|  | Cr | Cu | Mo | Nb | Ni | Ti | V |
|  | 0.30 | 0.30 | 0.08 | 0.005 | 0.50 | 0.03 | 0.10 |

- P355N Mechanical Property

| Grade |  | P355N Mechanical Property |
| --- | --- | --- |
|  | Thickness | Yield | Tensilmie | Elongation | Impact Energy(KV J) min |
| P355N | mm | Min Mpa | Mpa | Min % | -20° | 0° | +20° |
|  | ≤ 16 | 355 | 490-630 | 22 | 40 | 47 | 55 |
|  | 16> to ≤35 | 355 | 490-630 | 22 | 40 | 47 | 55 |
|  | 35> to ≤50 | 345 | 490-630 | 22 | 40 | 47 | 55 |
|  | 50> to ≤70 | 325 | 490-630 | 22 | 40 | 47 | 55 |
|  | 70> to ≤100 | 315 | 470-610 | 21 | 40 | 47 | 55 |
|  | 100> to ≤150 | 295 | 450-590 | 21 | 40 | 47 | 55 |

EN10028 steel grade supersedes the older BS and DIN standards. P355N steel grade is one of grade in EN10028-3, which is non alloy and alloy steels with specified elevated temperature properties. P355N grade are used above all for manufacturing boilers, pressure vessels and pipes transporting hot liquids.

- P355N Delivery Time Or Lead Time: 15-30days

- P355N Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for P355N, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting EN10028-3 P355N NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

P355N,P355N,P355N Steel Plate,P355N HIC, P355NNace

Tags: P355N,EN10028-3 P355N,P355N Steel Plate,P355N steel factory, P355N adopt standard, P355N Heat treatment, P355N Technical delivery condition, P355N Chemical, P355N Mechanical property, P355N Price, P355N CEV, P355N Impact degree, P355N impact energy, P355N Supplier,P355N Specification, P355N properties, Material P355N N, P355N Material, EN10028-3 P355N, P355N Steel, P355N Yield, P355N plate, P355N HIC, P355N NACE MR0175, P355N ISO 15156, P355N NACE MR0103, P355N SSC