P460NH MR0175,P460NH Steel plate,P460NH HIC,P460NH NACE

Gangsteel Bolier Plate Factory are specialized in producing and exporting EN10028-3 P460NH NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

P460NH,EN10028-3 P460NH,P460NH Steel Plate,P460NH HIC,P460NH Nace

Tags: P460NH,EN10028-3 P460NH,P460NH Steel Plate,P460NH steel factory, P460NH adopt standard, P460NH Heat treatment, P460NH Technical delivery condition, P460NH Chemical, P460NH Mechanical property, P460NH Price, P460NH CEV, P460NH Impact degree, P460NH impact energy, P460NH Supplier,P460NH Specification, P460NH properties, Material P460NH N, P460NH Material, EN10028-3 P460NH, P460NH Steel, P460NH Yield, P460NH plate, P460NH HIC, P460NH NACE MR0175, P460NH ISO 15156, P460NH NACE MR0103, P460NH SSC

Keyword: P460NH,EN10028-3 P460NH,P460NH Steel,P460NH HIC, P460NH NACE

- P460NH Adopt standard: EN10028-3 Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- P460NH Specification:  Thickness: 1mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for P460NH: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- P460NH Chemical composition % of the Product analysis of grade

| P460NH Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al(min) | N |
| P460NH | 0.20 | 0.60 | 1.0-1.70 | 0.030 | 0.020 |  | 0.025 |
|  | Cr | Cu | Mo | Nb | Ni | Ti | V |
|  | 0.30 | 0.70 | 0.10 | 0.005 | 0.80 | 0.03 | 0.20 |

- P460NH Mechanical Property

| Grade |  | P460NH Mechanical Property |
| --- | --- | --- |
|  | Thickness | Yield | Tensilmie | Elongation | Impact Energy(KV J) min |
| P460NH | mm | Min Mpa | Mpa | Min % | -20° | 0° | +20° |
|  | ≤ 16 | 460 | 570-720 | 17 | 47 | 55 | 63 |
|  | 16> to ≤35 | 450 | 570-720 | 17 | 47 | 55 | 63 |
|  | 35> to ≤50 | 440 | 570-720 | 17 | 47 | 55 | 63 |
|  | 50> to ≤70 | 420 | 570-720 | 17 | 47 | 55 | 63 |
|  | 70> to ≤100 | 400 | 540-710 | 16 | 47 | 55 | 63 |
|  | 100> to ≤150 | 380 | 520-690 | 16 | 47 | 55 | 63 |

EN10028 steel grade supersedes the older BS and DIN standards. P460NH steel grade is one of grade in EN10028-3, which is non alloy and alloy steels with specified elevated temperature properties. P460NH grade are used above all for manufacturing boilers, pressure vessels and pipes transporting hot liquids.

- P460NH Delivery Time Or Lead Time: 15-30days

- P460NH Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for P460NH, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting EN10028-3 P460NH NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

P460NH,P460NH,P460NH Steel Plate,P460NH HIC, P460NHNace

Tags: P460NH,EN10028-3 P460NH,P460NH Steel Plate,P460NH steel factory, P460NH adopt standard, P460NH Heat treatment, P460NH Technical delivery condition, P460NH Chemical, P460NH Mechanical property, P460NH Price, P460NH CEV, P460NH Impact degree, P460NH impact energy, P460NH Supplier,P460NH Specification, P460NH properties, Material P460NH N, P460NH Material, EN10028-3 P460NH, P460NH Steel, P460NH Yield, P460NH plate, P460NH HIC, P460NH NACE MR0175, P460NH ISO 15156, P460NH NACE MR0103, P460NH SSC