P460N MR0175,P460N Steel plate,P460N HIC,P460N NACE

Gangsteel Bolier Plate Factory are specialized in producing and exporting EN10028-3 P460N NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

P460N,EN10028-3 P460N,P460N Steel Plate,P460N HIC,P460N Nace

Tags: P460N,EN10028-3 P460N,P460N Steel Plate,P460N steel factory, P460N adopt standard, P460N Heat treatment, P460N Technical delivery condition, P460N Chemical, P460N Mechanical property, P460N Price, P460N CEV, P460N Impact degree, P460N impact energy, P460N Supplier,P460N Specification, P460N properties, Material P460N N, P460N Material, EN10028-3 P460N, P460N Steel, P460N Yield, P460N plate, P460N HIC, P460N NACE MR0175, P460N ISO 15156, P460N NACE MR0103, P460N SSC

Keyword: P460N,EN10028-3 P460N,P460N Steel,P460N HIC, P460N NACE

- P460N Adopt standard: EN10028-3 Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- P460N Specification:  Thickness: 1mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for P460N: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- P460N Chemical composition % of the Product analysis of grade

| P460N Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al(min) | N |
| P460N | 0.20 | 0.60 | 1.0-1.70 | 0.030 | 0.025 |  | 0.025 |
|  | Cr | Cu | Mo | Nb | Ni | Ti | V |
|  | 0.30 | 0.70 | 0.10 | 0.005 | 0.80 | 0.03 | 0.20 |

- P460N Mechanical Property

| Grade |  | P460N Mechanical Property |
| --- | --- | --- |
|  | Thickness | Yield | Tensilmie | Elongation | Impact Energy(KV J) min |
| P460N | mm | Min Mpa | Mpa | Min % | -20° | 0° | +20° |
|  | ≤ 16 | 460 | 570-720 | 17 | 40 | 47 | 55 |
|  | 16> to ≤35 | 450 | 570-720 | 17 | 40 | 47 | 55 |
|  | 35> to ≤50 | 440 | 570-720 | 17 | 40 | 47 | 55 |
|  | 50> to ≤70 | 420 | 570-720 | 17 | 40 | 47 | 55 |
|  | 70> to ≤100 | 400 | 540-710 | 16 | 40 | 47 | 55 |
|  | 100> to ≤150 | 380 | 520-690 | 16 | 40 | 47 | 55 |

EN10028 steel grade supersedes the older BS and DIN standards. P460N steel grade is one of grade in EN10028-3, which is non alloy and alloy steels with specified elevated temperature properties. P460N grade are used above all for manufacturing boilers, pressure vessels and pipes transporting hot liquids.

- P460N Delivery Time Or Lead Time: 15-30days

- P460N Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for P460N, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting EN10028-3 P460N NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

P460N,P460N,P460N Steel Plate,P460N HIC, P460NNace

Tags: P460N,EN10028-3 P460N,P460N Steel Plate,P460N steel factory, P460N adopt standard, P460N Heat treatment, P460N Technical delivery condition, P460N Chemical, P460N Mechanical property, P460N Price, P460N CEV, P460N Impact degree, P460N impact energy, P460N Supplier,P460N Specification, P460N properties, Material P460N N, P460N Material, EN10028-3 P460N, P460N Steel, P460N Yield, P460N plate, P460N HIC, P460N NACE MR0175, P460N ISO 15156, P460N NACE MR0103, P460N SSC