A202GRA,A202GRA Steel Plate,A202GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A202/A202M A202GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A202GRA,A202/A202M A202GRA,A202GRA Steel Plate,A202GRA HIC,A202GRA Nace

Tags: A202GRA,A202/A202M A202GRA,A202GRA Steel Plate,A202GRA steel factory, A202GRA adopt standard, A202GRA Heat treatment, A202GRA Technical delivery condition, A202GRA Chemical, A202GRA Mechanical property, A202GRA Price, A202GRA CEV, A202GRA Impact degree, A202GRA impact energy, A202GRA Supplier,A202GRA Specification, A202GRA properties, Material A202GRA N, A202GRA Material, A202/A202M, A202GRA Steel, A202GRA Yield, A202GRA plate, A202GRA HIC, A202GRA NACE MR0175, A202GRA ISO 15156, A202GRA NACE MR0103, A202GRA SSC

Keyword: A202GRA,A202GRA Steel Plate,A202GRA Supplier

1.  A202GRA Adopt standard: ASMT A202/A202M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  A202GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A202GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A202GRA Chemical composition % of the Product analysis of grade

| Grade | C % | P % | S% | Si% | Cr% | Mn% |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A202GRA | 0.17 | 0.035 | 0.035 | 0.54-0.96 | 0.31-0.64 | 0.97-1.52 |  |  |

5.  A202GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A202GRA | 310 Mpa | 515-655Mpa | <=50MM | 19% |
|  | 310 Mpa | 515-655Mpa | 50-200MM | 16% |

6.  Normally A202/A202M A202GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A202GRA Delivery Time Or Lead Time: 20-35days

8.  A202GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A202GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A202/A202M A202GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A202GRA,A202/A202M A202GRA,A202GRA Steel Plate,A202GRA HIC,A202GRA Nace

Tags: A202GRA,A202/A202M A202GRA,A202GRA Steel Plate,A202GRA steel factory, A202GRA adopt standard, A202GRA Heat treatment, A202GRA Technical delivery condition, A202GRA Chemical, A202GRA Mechanical property, A202GRA Price, A202GRA CEV, A202GRA Impact degree, A202GRA impact energy, A202GRA Supplier,A202GRA Specification, A202GRA properties, Material A202GRA N, A202GRA Material, A202/A202M, A202GRA Steel, A202GRA Yield, A202GRA plate, A202GRA HIC, A202GRA NACE MR0175, A202GRA ISO 15156, A202GRA NACE MR0103, A202GRA SSC