GB/T 19189 12MnNiVR, 12MnNiVR STEEL PLATE,12MnNiVR Boiler steel plate

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 19189 12MnNiVR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,Quenched and tempered high strength steel plates for pressure vessels,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

12MnNiVR,GB/T 19189 12MnNiVR,12MnNiVR Steel Plate,12MnNiVR HIC,12MnNiVR Nace

Tags: 12MnNiVR,GB/T 19189 12MnNiVR,12MnNiVR Steel Plate,12MnNiVR steel factory, 12MnNiVR adopt standard, 12MnNiVR Heat treatment, 12MnNiVR Technical delivery condition, 12MnNiVR Chemical, 12MnNiVR Mechanical property, 12MnNiVR Price, 12MnNiVR CEV, 12MnNiVR Impact degree, 12MnNiVR impact energy, 12MnNiVR Supplier,12MnNiVR Specification, 12MnNiVR properties, Material 12MnNiVR N, 12MnNiVR Material, GB/T 19189, 12MnNiVR Steel, 12MnNiVR Yield, 12MnNiVR plate, 12MnNiVR HIC, 12MnNiVR NACE MR0175, 12MnNiVR ISO 15156, 12MnNiVR NACE MR0103, 12MnNiVR SSC

Keyword: 12MnNiVR,GB/T 19189 12MnNiVR,12MnNiVR Steel,12MnNiVR HIC,12MnNiVR NACE

1.  12MnNiVR Adopt standard: GB/T 19189Quenched and tempered high strength steel plates for pressure vessels.

2.  12MnNiVR Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for 12MnNiVR: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  12MnNiVR Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | P% | S% | Cu% | Ni% | Cr% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 12MnNiVR | 0.15 | 0.15-0.4 | 1.2-1.6 | 0.02 | 0.01 | 0.25 | 0.15-0.40 | 0.30 |
|  | Mo% | V% | B % | Pcm% |  |  |  |  |
|  | 0.3 | 0.02-0.06 | 0.002 | 0.25 |  |  |  |  |

5.  12MnNiVR Mechanical Property

| Grade | Thickness(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| 12MnNiVR |  |  |  |  | Degree | Min J |
|  | 10-60 | 490 Mpa | 610-730 Mpa | 17% | -20 | 80J |

6.  Normally GB/T 19189 12MnNiVR plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  12MnNiVR Delivery Time Or Lead Time: 20-35days

8.  12MnNiVR Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for 12MnNiVR, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 19189 12MnNiVR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

12MnNiVR,GB/T 19189 12MnNiVR,12MnNiVR Steel Plate,12MnNiVR HIC,12MnNiVR Nace

Tags: 12MnNiVR,GB/T 19189 12MnNiVR,12MnNiVR Steel Plate,12MnNiVR steel factory, 12MnNiVR adopt standard, 12MnNiVR Heat treatment, 12MnNiVR Technical delivery condition, 12MnNiVR Chemical, 12MnNiVR Mechanical property, 12MnNiVR Price, 12MnNiVR CEV, 12MnNiVR Impact degree, 12MnNiVR impact energy, 12MnNiVR Supplier,12MnNiVR Specification, 12MnNiVR properties, Material 12MnNiVR N, 12MnNiVR Material, GB/T 19189, 12MnNiVR Steel, 12MnNiVR Yield, 12MnNiVR plate, 12MnNiVR HIC, 12MnNiVR NACE MR0175, 12MnNiVR ISO 15156, 12MnNiVR NACE MR0103, 12MnNiVR SSC