A387GR21L,A387GR21L Steel Plate,A387GR21L Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR21L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. A387GR21L,A387/A387M A387GR21L,A387GR21L Steel Plate,A387GR21L HIC,A387GR21L Nace

Tags: A387GR21L,A387/A387M A387GR21L,A387GR21L Steel Plate,A387GR21L steel factory, A387GR21L adopt standard, A387GR21L Heat treatment, A387GR21L Technical delivery condition, A387GR21L Chemical, A387GR21L Mechanical property, A387GR21L Price, A387GR21L CEV, A387GR21L Impact degree, A387GR21L impact energy, A387GR21L Supplier,A387GR21L Specification, A387GR21L properties, Material A387GR21L N, A387GR21L Material, A387/A387M, A387GR21L Steel, A387GR21L Yield, A387GR21L plate, A387GR21L HIC, A387GR21L NACE MR0175, A387GR21L ISO 15156, A387GR21L NACE MR0103, A387GR21L SSC

Keyword: A387GR21L,A387GR21L Steel Plate,A387GR21L Supplier

1.  A387GR21L Adopt standard: ASMT A387/A387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  A387GR21L Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A387GR21L: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A387GR21L Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A387GR21L | 0.12 | 0.25-0.66 | 0.035 | 0.035 | 0.5 | 2.63-3.37 | 0.85-1.15 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  A387GR21L Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A387GR21L | 205Mpa | 415-585Mpa | <=50MM | 18% |
|  | 205Mpa | 415-585Mpa | 50-200MM | -- |

6.  Normally A387/A387M A387GR21L plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A387GR21L Delivery Time Or Lead Time: 20-35days

8.  A387GR21L Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A387GR21L, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR21L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A387GR21L,A387/A387M A387GR21L,A387GR21L Steel Plate,A387GR21L HIC,A387GR21L Nace

Tags: A387GR21L,A387/A387M A387GR21L,A387GR21L Steel Plate,A387GR21L steel factory, A387GR21L adopt standard, A387GR21L Heat treatment, A387GR21L Technical delivery condition, A387GR21L Chemical, A387GR21L Mechanical property, A387GR21L Price, A387GR21L CEV, A387GR21L Impact degree, A387GR21L impact energy, A387GR21L Supplier,A387GR21L Specification, A387GR21L properties, Material A387GR21L N, A387GR21L Material, A387/A387M, A387GR21L Steel, A387GR21L Yield, A387GR21L plate, A387GR21L HIC, A387GR21L NACE MR0175, A387GR21L ISO 15156, A387GR21L NACE MR0103, A387GR21L SSC