A533CL3,A533CL3 Steel Plate,A533CL3 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A533/A533M A533CL3 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for pressure Vessel Plates,Alloy Steel,Quenched and tempered,Manganese-Molybdenum and Manganese-Molybdenum-Nickel Which is a large steel plate supplier mill at Gangsteel Group. A533CL3,A533/A533M A533CL3,A533CL3 Steel Plate,A533CL3 HIC,A533CL3 Nace

Tags: A533CL3,A533/A533M A533CL3,A533CL3 Steel Plate,A533CL3 steel factory, A533CL3 adopt standard, A533CL3 Heat treatment, A533CL3 Technical delivery condition, A533CL3 Chemical, A533CL3 Mechanical property, A533CL3 Price, A533CL3 CEV, A533CL3 Impact degree, A533CL3 impact energy, A533CL3 Supplier,A533CL3 Specification, A533CL3 properties, Material A533CL3 N, A533CL3 Material, A533/A533M, A533CL3 Steel, A533CL3 Yield, A533CL3 plate, A533CL3 HIC, A533CL3 NACE MR0175, A533CL3 ISO 15156, A533CL3 NACE MR0103, A533CL3 SSC

Keyword: A533CL3,A533CL3 Steel Plate,A533CL3 Supplier

1.  A533CL3 Adopt standard: ASMT A533/A533MStandard Specification for pressure Vessel Plates,Alloy Steel,Quenched and tempered,Manganese-Molybdenum and Manganese-Molybdenum-Nickel

2.  A533CL3 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A533CL3: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A533CL3 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A533CL3 | 0.25 | 1.07-1.82 | 0.035 | 0.035 | 0.13-0.45 | 0.41-0.84 | 0.67-1.03 |

5.  A533CL3 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A533CL3 | 570 Mpa | 690-860Mpa | <50MM | 16% |

6.  Normally A533/A533M A533CL3 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A533CL3 Delivery Time Or Lead Time: 20-35days

8.  A533CL3 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A533CL3, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A533/A533MA533CL3 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A533CL3,A533/A533M A533CL3,A533CL3 Steel Plate,A533CL3 HIC,A533CL3 Nace

Tags: A533CL3,A533/A533M A533CL3,A533CL3 Steel Plate,A533CL3 steel factory, A533CL3 adopt standard, A533CL3 Heat treatment, A533CL3 Technical delivery condition, A533CL3 Chemical, A533CL3 Mechanical property, A533CL3 Price, A533CL3 CEV, A533CL3 Impact degree, A533CL3 impact energy, A533CL3 Supplier,A533CL3 Specification, A533CL3 properties, Material A533CL3 N, A533CL3 Material, A533/A533M, A533CL3 Steel, A533CL3 Yield, A533CL3 plate, A533CL3 HIC, A533CL3 NACE MR0175, A533CL3 ISO 15156, A533CL3 NACE MR0103, A533CL3 SSC