A710CL1,A710CL1 Steel Plate,A710CL1 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A710/A710M A710CL1 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates, Which is a large steel plate supplier mill at Gangsteel Group. A710CL1,A710/A710M A710CL1,A710CL1 Steel Plate,A710CL1 HIC,A710CL1 Nace

Tags: A710CL1,A710/A710M A710CL1,A710CL1 Steel Plate,A710CL1 steel factory, A710CL1 adopt standard, A710CL1 Heat treatment, A710CL1 Technical delivery condition, A710CL1 Chemical, A710CL1 Mechanical property, A710CL1 Price, A710CL1 CEV, A710CL1 Impact degree, A710CL1 impact energy, A710CL1 Supplier,A710CL1 Specification, A710CL1 properties, Material A710CL1 N, A710CL1 Material, A710/A710M, A710CL1 Steel, A710CL1 Yield, A710CL1 plate, A710CL1 HIC, A710CL1 NACE MR0175, A710CL1 ISO 15156, A710CL1 NACE MR0103, A710CL1 SSC

Keyword: A710CL1,A710CL1 Steel Plate,A710CL1 Supplier

1.  A710CL1 Adopt standard: ASMT A710/A710M Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates.

2.  A710CL1 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A710CL1: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A710CL1 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Ni% |
| --- | --- | --- | --- | --- | --- | --- |
| A710CL1 | 0.07 | 0.40-0.70 | 0.025 | 0.025 | 0.4 | 0.7-1.0 |
|  | Mo% | Cu% | Cb% | Ti% | Cr% |  |
|  | 0.15-0.25 | 1.0-1.3 | 0.02 | -- | 0.6-0.9 |  |

5.  A710CL1 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A710CL1 | 585Mpa | 620Mpa | <6.5mm | 20% |
|  | 585Mpa | 620Mpa | 6.5-8mm | 20% |
|  | 550Mpa | 620Mpa | 8-10mm | 20% |
|  | 550Mpa | 620Mpa | 10-12.5mm | 20% |
|  | 550Mpa | 620Mpa | 12.5-20mm | 20% |
|  | --- | -- | 20-25mm | 20% |
|  | --- | --- | 25-30mm | 20% |
|  | --- | --- | 30-50mm | 20% |
|  | --- | --- | 50-100mm | -- |
|  | --- | --- | >100mm | -- |

6.  Normally A710/A710M A710CL1 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A710CL1 Delivery Time Or Lead Time: 20-35days

8.  A710CL1 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A710CL1, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A710/A710MA710CL1 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A710CL1,A710/A710M A710CL1,A710CL1 Steel Plate,A710CL1 HIC,A710CL1 Nace

Tags: A710CL1,A710/A710M A710CL1,A710CL1 Steel Plate,A710CL1 steel factory, A710CL1 adopt standard, A710CL1 Heat treatment, A710CL1 Technical delivery condition, A710CL1 Chemical, A710CL1 Mechanical property, A710CL1 Price, A710CL1 CEV, A710CL1 Impact degree, A710CL1 impact energy, A710CL1 Supplier,A710CL1 Specification, A710CL1 properties, Material A710CL1 N, A710CL1 Material, A710/A710M, A710CL1 Steel, A710CL1 Yield, A710CL1 plate, A710CL1 HIC, A710CL1 NACE MR0175, A710CL1 ISO 15156, A710CL1 NACE MR0103, A710CL1 SSC