A738GRA,A738GRA Steel Plate,A738GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M A738GRA NACE MR0175, MR0103 Boiler steel plate, Specification for pressure plates,heat-treated,carbon-manganese-silicon steel ,for moderate and lower temperature service. Which is a large steel plate supplier mill at Gangsteel Group. A738GRA,SA-738/SA-738M A738GRA,A738GRA Steel Plate,A738GRA HIC,A738GRA Nace

Tags: A738GRA,SA-738/SA-738M A738GRA,A738GRA Steel Plate,A738GRA steel factory, A738GRA adopt standard, A738GRA Heat treatment, A738GRA Technical delivery condition, A738GRA Chemical, A738GRA Mechanical property, A738GRA Price, A738GRA CEV, A738GRA Impact degree, A738GRA impact energy, A738GRA Supplier,A738GRA Specification, A738GRA properties, Material A738GRA N, A738GRA Material, SA-738/SA-738M, A738GRA Steel, A738GRA Yield, A738GRA plate, A738GRA HIC, A738GRA NACE MR0175, A738GRA ISO 15156, A738GRA NACE MR0103, A738GRA SSC

Keyword: A738GRA,A738GRA Steel Plate,A738GRA Supplier

1.  A738GRA Adopt standard: ASMT SA-738/SA-738M Specification for pressure plates,heat-treated,carbon-manganese-silicon steel.

2.  A738GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A738GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A738GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<65mm) | Mn %(>65mm) | P% | S% | Si% | Cu% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A738GRA | 0.24 | 1.62 | 1.72 | 0.035 | 0.035 | 0.13-0.55 | 0.38 | 0.53 |
|  | Cr% | Mo%(40mm) | Mo%(<40mm) | V% | Cb% | Cb plus V |  |  |
|  | 0.29 | 0.08 | 0.08 | 0.08 | 0.05 | 0.10 |  |  |

5.  A738GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A738GRA | 310 Mpa | 515-655Mpa | <65MM | 20% |
|  | 310 Mpa | 515-655Mpa | 65-100MM | 20% |
|  | 310 Mpa | 515-655Mpa | >100MM | 20% |

6.  Normally SA-738/SA-738M A738GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A738GRA Delivery Time Or Lead Time: 20-35days

8.  A738GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A738GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M A738GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A738GRA,SA-738/SA-738M A738GRA,A738GRA Steel Plate,A738GRA HIC,A738GRA Nace

Tags: A738GRA,SA-738/SA-738M A738GRA,A738GRA Steel Plate,A738GRA steel factory, A738GRA adopt standard, A738GRA Heat treatment, A738GRA Technical delivery condition, A738GRA Chemical, A738GRA Mechanical property, A738GRA Price, A738GRA CEV, A738GRA Impact degree, A738GRA impact energy, A738GRA Supplier,A738GRA Specification, A738GRA properties, Material A738GRA N, A738GRA Material, SA-738/SA-738M, A738GRA Steel, A738GRA Yield, A738GRA plate, A738GRA HIC, A738GRA NACE MR0175, A738GRA ISO 15156, A738GRA NACE MR0103, A738GRA SSC