A738 GRADE B,A738 GRADE B Steel Plate,A738 GRADE B Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M A738 GRADE B NACE MR0175, MR0103 Boiler steel plate, Specification for pressure plates,heat-treated,carbon-manganese-silicon steel ,for moderate and lower temperature service. Which is a large steel plate supplier mill at Gangsteel Group. A738 GRADE B,SA-738/SA-738M A738 GRADE B,A738 GRADE B Steel Plate,A738 GRADE B HIC,A738 GRADE B Nace

Tags: A738 GRADE B,SA-738/SA-738M A738 GRADE B,A738 GRADE B Steel Plate,A738 GRADE B steel factory, A738 GRADE B adopt standard, A738 GRADE B Heat treatment, A738 GRADE B Technical delivery condition, A738 GRADE B Chemical, A738 GRADE B Mechanical property, A738 GRADE B Price, A738 GRADE B CEV, A738 GRADE B Impact degree, A738 GRADE B impact energy, A738 GRADE B Supplier,A738 GRADE B Specification, A738 GRADE B properties, Material A738 GRADE B N, A738 GRADE B Material, SA-738/SA-738M, A738 GRADE B Steel, A738 GRADE B Yield, A738 GRADE B plate, A738 GRADE B HIC, A738 GRADE B NACE MR0175, A738 GRADE B ISO 15156, A738 GRADE B NACE MR0103, A738 GRADE B SSC

Keyword: A738 GRADE B,A738 GRADE B Steel Plate,A738 GRADE B Supplier

1.  A738 GRADE B Adopt standard: ASMT SA-738/SA-738M Specification for pressure plates,heat-treated,carbon-manganese-silicon steel.

2.  A738 GRADE B Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A738 GRADE B: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A738 GRADE B Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<65mm) | Mn %(>65mm) | P% | S% | Si% | Cu% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A738 GRADE B | 0.20 | 0.84-1.62 | 0.84-1.72 | 0.030 | 0.030 | 0.13-0.60 | 0.38 | 0.63 |
|  | Cr% | Mo%(40mm) | Mo%(<40mm) | V% | Cb% | Cb plus V |  |  |
|  | 0.34 | 0.30 | 0.33 | 0.08 | 0.05 | 0.10 |  |  |

5.  A738 GRADE B Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A738 GRADE B | 415 Mpa | 585-705Mpa | <65MM | 20% |
|  | 415 Mpa | 585-705Mpa | 65-100MM | 20% |
|  | 415 Mpa | 585-705Mpa | >100MM | 20% |

6.  Normally SA-738/SA-738M A738 GRADE B plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A738 GRADE B Delivery Time Or Lead Time: 20-35days

8.  A738 GRADE B Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A738 GRADE B, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M A738 GRADE B NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A738 GRADE B,SA-738/SA-738M A738 GRADE B,A738 GRADE B Steel Plate,A738 GRADE B HIC,A738 GRADE B Nace

Tags: A738 GRADE B,SA-738/SA-738M A738 GRADE B,A738 GRADE B Steel Plate,A738 GRADE B steel factory, A738 GRADE B adopt standard, A738 GRADE B Heat treatment, A738 GRADE B Technical delivery condition, A738 GRADE B Chemical, A738 GRADE B Mechanical property, A738 GRADE B Price, A738 GRADE B CEV, A738 GRADE B Impact degree, A738 GRADE B impact energy, A738 GRADE B Supplier,A738 GRADE B Specification, A738 GRADE B properties, Material A738 GRADE B N, A738 GRADE B Material, SA-738/SA-738M, A738 GRADE B Steel, A738 GRADE B Yield, A738 GRADE B plate, A738 GRADE B HIC, A738 GRADE B NACE MR0175, A738 GRADE B ISO 15156, A738 GRADE B NACE MR0103, A738 GRADE B SSC