A738GRB,A738GRB Steel Plate,A738GRB Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M A738GRB NACE MR0175, MR0103 Boiler steel plate, Specification for pressure plates,heat-treated,carbon-manganese-silicon steel ,for moderate and lower temperature service. Which is a large steel plate supplier mill at Gangsteel Group. A738GRB,SA-738/SA-738M A738GRB,A738GRB Steel Plate,A738GRB HIC,A738GRB Nace

Tags: A738GRB,SA-738/SA-738M A738GRB,A738GRB Steel Plate,A738GRB steel factory, A738GRB adopt standard, A738GRB Heat treatment, A738GRB Technical delivery condition, A738GRB Chemical, A738GRB Mechanical property, A738GRB Price, A738GRB CEV, A738GRB Impact degree, A738GRB impact energy, A738GRB Supplier,A738GRB Specification, A738GRB properties, Material A738GRB N, A738GRB Material, SA-738/SA-738M, A738GRB Steel, A738GRB Yield, A738GRB plate, A738GRB HIC, A738GRB NACE MR0175, A738GRB ISO 15156, A738GRB NACE MR0103, A738GRB SSC

Keyword: A738GRB,A738GRB Steel Plate,A738GRB Supplier

1.  A738GRB Adopt standard: ASMT SA-738/SA-738M Specification for pressure plates,heat-treated,carbon-manganese-silicon steel.

2.  A738GRB Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A738GRB: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A738GRB Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<65mm) | Mn %(>65mm) | P% | S% | Si% | Cu% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A738GRB | 0.20 | 0.84-1.62 | 0.84-1.72 | 0.030 | 0.030 | 0.13-0.60 | 0.38 | 0.63 |
|  | Cr% | Mo%(40mm) | Mo%(<40mm) | V% | Cb% | Cb plus V |  |  |
|  | 0.34 | 0.30 | 0.33 | 0.08 | 0.05 | 0.10 |  |  |

5.  A738GRB Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A738GRB | 415 Mpa | 585-705Mpa | <65MM | 20% |
|  | 415 Mpa | 585-705Mpa | 65-100MM | 20% |
|  | 415 Mpa | 585-705Mpa | >100MM | 20% |

6.  Normally SA-738/SA-738M A738GRB plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A738GRB Delivery Time Or Lead Time: 20-35days

8.  A738GRB Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A738GRB, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M A738GRB NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A738GRB,SA-738/SA-738M A738GRB,A738GRB Steel Plate,A738GRB HIC,A738GRB Nace

Tags: A738GRB,SA-738/SA-738M A738GRB,A738GRB Steel Plate,A738GRB steel factory, A738GRB adopt standard, A738GRB Heat treatment, A738GRB Technical delivery condition, A738GRB Chemical, A738GRB Mechanical property, A738GRB Price, A738GRB CEV, A738GRB Impact degree, A738GRB impact energy, A738GRB Supplier,A738GRB Specification, A738GRB properties, Material A738GRB N, A738GRB Material, SA-738/SA-738M, A738GRB Steel, A738GRB Yield, A738GRB plate, A738GRB HIC, A738GRB NACE MR0175, A738GRB ISO 15156, A738GRB NACE MR0103, A738GRB SSC