A738GRC,A738GRC Steel Plate,A738GRC Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M A738GRC NACE MR0175, MR0103 Boiler steel plate, Specification for pressure plates,heat-treated,carbon-manganese-silicon steel ,for moderate and lower temperature service. Which is a large steel plate supplier mill at Gangsteel Group. A738GRC,SA-738/SA-738M A738GRC,A738GRC Steel Plate,A738GRC HIC,A738GRC Nace

Tags: A738GRC,SA-738/SA-738M A738GRC,A738GRC Steel Plate,A738GRC steel factory, A738GRC adopt standard, A738GRC Heat treatment, A738GRC Technical delivery condition, A738GRC Chemical, A738GRC Mechanical property, A738GRC Price, A738GRC CEV, A738GRC Impact degree, A738GRC impact energy, A738GRC Supplier,A738GRC Specification, A738GRC properties, Material A738GRC N, A738GRC Material, SA-738/SA-738M, A738GRC Steel, A738GRC Yield, A738GRC plate, A738GRC HIC, A738GRC NACE MR0175, A738GRC ISO 15156, A738GRC NACE MR0103, A738GRC SSC

Keyword: A738GRC,A738GRC Steel Plate,A738GRC Supplier

1.  A738GRC Adopt standard: ASMT SA-738/SA-738M Specification for pressure plates,heat-treated,carbon-manganese-silicon steel.

2.  A738GRC Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A738GRC: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A738GRC Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<65mm) | Mn %(>65mm) | P% | S% | Si% | Cu% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A738GRC | 0.24 | 1.62 | 1.72 | 0.025 | 0.025 | 0.13-0.55 | 0.38 | 0.53 |
|  | Cr% | Mo%(40mm) | Mo%(<40mm) | V% | Cb% | Cb plus V |  |  |
|  | 0.29 | 0.08 | 0.08 | 0.05 | -- | -- |  |  |

5.  A738GRC Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A738GRC | 415 Mpa | 550-690Mpa | <65MM | 22% |
|  | 380 Mpa | 515-655Mpa | 65-100MM | 22% |
|  | 315 Mpa | 485-655Mpa | >100MM | 20% |

6.  Normally SA-738/SA-738M A738GRC plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A738GRC Delivery Time Or Lead Time: 20-35days

8.  A738GRC Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A738GRC, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M A738GRC NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A738GRC,SA-738/SA-738M A738GRC,A738GRC Steel Plate,A738GRC HIC,A738GRC Nace

Tags: A738GRC,SA-738/SA-738M A738GRC,A738GRC Steel Plate,A738GRC steel factory, A738GRC adopt standard, A738GRC Heat treatment, A738GRC Technical delivery condition, A738GRC Chemical, A738GRC Mechanical property, A738GRC Price, A738GRC CEV, A738GRC Impact degree, A738GRC impact energy, A738GRC Supplier,A738GRC Specification, A738GRC properties, Material A738GRC N, A738GRC Material, SA-738/SA-738M, A738GRC Steel, A738GRC Yield, A738GRC plate, A738GRC HIC, A738GRC NACE MR0175, A738GRC ISO 15156, A738GRC NACE MR0103, A738GRC SSC