A841-2,A841-2 Steel Plate,A841-2 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M A841-2 NACE MR0175, MR0103 Boiler steel plate, Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP) Which is a large steel plate supplier mill at Gangsteel Group. A841-2,SA-841/SA-841M A841-2,A841-2 Steel Plate,A841-2 HIC,A841-2 Nace

Tags: A841-2,SA-841/SA-841M A841-2,A841-2 Steel Plate,A841-2 steel factory, A841-2 adopt standard, A841-2 Heat treatment, A841-2 Technical delivery condition, A841-2 Chemical, A841-2 Mechanical property, A841-2 Price, A841-2 CEV, A841-2 Impact degree, A841-2 impact energy, A841-2 Supplier,A841-2 Specification, A841-2 properties, Material A841-2 N, A841-2 Material, SA-841/SA-841M, A841-2 Steel, A841-2 Yield, A841-2 plate, A841-2 HIC, A841-2 NACE MR0175, A841-2 ISO 15156, A841-2 NACE MR0103, A841-2 SSC

Keyword: A841-2,A841-2 Steel Plate,A841-2 Supplier

1.  A841-2 Adopt standard: ASMT SA-841/SA-841M Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP)

2.  A841-2 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A841-2: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A841-2 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Cu% | Ni% | Cr% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A841-2 | 0.15 | 0.7-1.35 | 0.03 | 0.025 | 0.15-0.5 | 0.35 | 0.6 | 0.25 |
|  | Mo% | Cb% | V% | Mn %(>40mm) | Ti% | B% |  |  |
|  | 0.3 | 0.03 | 0.06 | 1.0-1.6 | -- | -- |  |  |

4.  A841-2 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A841-2 | 415 Mpa | 550-690Mpa | <40MM | 22% |
|  | 415 Mpa | 550-690Mpa | 40-65MM | 22% |
|  | 380 Mpa | 515-655Mpa | >65MM | 22% |

5.  Normally SA-841/SA-841M A841-2 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

6.  A841-2 Delivery Time Or Lead Time: 20-35days

7.  A841-2 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

8.  If you have any requirement in steel plate for A841-2, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M A841-2 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A841-2,SA-841/SA-841M A841-2,A841-2 Steel Plate,A841-2 HIC,A841-2 Nace

Tags: A841-2,SA-841/SA-841M A841-2,A841-2 Steel Plate,A841-2 steel factory, A841-2 adopt standard, A841-2 Heat treatment, A841-2 Technical delivery condition, A841-2 Chemical, A841-2 Mechanical property, A841-2 Price, A841-2 CEV, A841-2 Impact degree, A841-2 impact energy, A841-2 Supplier,A841-2 Specification, A841-2 properties, Material A841-2 N, A841-2 Material, SA-841/SA-841M, A841-2 Steel, A841-2 Yield, A841-2 plate, A841-2 HIC, A841-2 NACE MR0175, A841-2 ISO 15156, A841-2 NACE MR0103, A841-2 SSC