A841 GRADE A,A841 GRADE A Steel Plate,A841 GRADE A Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M A841 GRADE A NACE MR0175, MR0103 Boiler steel plate, Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP) Which is a large steel plate supplier mill at Gangsteel Group. A841 GRADE A,SA-841/SA-841M A841 GRADE A,A841 GRADE A Steel Plate,A841 GRADE A HIC,A841 GRADE A Nace

Tags: A841 GRADE A,SA-841/SA-841M A841 GRADE A,A841 GRADE A Steel Plate,A841 GRADE A steel factory, A841 GRADE A adopt standard, A841 GRADE A Heat treatment, A841 GRADE A Technical delivery condition, A841 GRADE A Chemical, A841 GRADE A Mechanical property, A841 GRADE A Price, A841 GRADE A CEV, A841 GRADE A Impact degree, A841 GRADE A impact energy, A841 GRADE A Supplier,A841 GRADE A Specification, A841 GRADE A properties, Material A841 GRADE A N, A841 GRADE A Material, SA-841/SA-841M, A841 GRADE A Steel, A841 GRADE A Yield, A841 GRADE A plate, A841 GRADE A HIC, A841 GRADE A NACE MR0175, A841 GRADE A ISO 15156, A841 GRADE A NACE MR0103, A841 GRADE A SSC

Keyword: A841 GRADE A,A841 GRADE A Steel Plate,A841 GRADE A Supplier

1.  A841 GRADE A Adopt standard: ASMT SA-841/SA-841M Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP)

2.  A841 GRADE A Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A841 GRADE A: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A841 GRADE A Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Cu% | Ni% | Cr% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A841 GRADE A | 0.2 | 0.7-1.35 | 0.03 | 0.03 | 0.15-0.5 | 0.35 | 0.25 | 0.25 |
|  | Mo% | Cb% | V% | Mn %(>40mm) | Ti% | B% |  |  |
|  | 0.08 | 0.03 | 0.06 | 1.0-1.6 | -- | -- |  |  |

5.  A841 GRADE A Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A841 GRADE A | 345 Mpa | 480-620Mpa | <40MM | 22% |
|  | 345 Mpa | 480-620Mpa | 40-65MM | 22% |
|  | 310 Mpa | 450-585Mpa | >65MM | 22% |

6.  Normally SA-841/SA-841M A841 GRADE A plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A841 GRADE A Delivery Time Or Lead Time: 20-35days

8.  A841 GRADE A Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A841 GRADE A, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M A841 GRADE A NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A841 GRADE A,SA-841/SA-841M A841 GRADE A,A841 GRADE A Steel Plate,A841 GRADE A HIC,A841 GRADE A Nace

Tags: A841 GRADE A,SA-841/SA-841M A841 GRADE A,A841 GRADE A Steel Plate,A841 GRADE A steel factory, A841 GRADE A adopt standard, A841 GRADE A Heat treatment, A841 GRADE A Technical delivery condition, A841 GRADE A Chemical, A841 GRADE A Mechanical property, A841 GRADE A Price, A841 GRADE A CEV, A841 GRADE A Impact degree, A841 GRADE A impact energy, A841 GRADE A Supplier,A841 GRADE A Specification, A841 GRADE A properties, Material A841 GRADE A N, A841 GRADE A Material, SA-841/SA-841M, A841 GRADE A Steel, A841 GRADE A Yield, A841 GRADE A plate, A841 GRADE A HIC, A841 GRADE A NACE MR0175, A841 GRADE A ISO 15156, A841 GRADE A NACE MR0103, A841 GRADE A SSC