SA283GRB,SA283GRB Steel Plate,SA283GRB Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA283/SA283M SA283GRB NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA283GRB,SA283/SA283M SA283GRB,SA283GRB Steel Plate,SA283GRB HIC,SA283GRB Nace

Tags: SA283GRB,SA283/SA283M SA283GRB,SA283GRB Steel Plate,SA283GRB steel factory, SA283GRB adopt standard, SA283GRB Heat treatment, SA283GRB Technical delivery condition, SA283GRB Chemical, SA283GRB Mechanical property, SA283GRB Price, SA283GRB CEV, SA283GRB Impact degree, SA283GRB impact energy, SA283GRB Supplier,SA283GRB Specification, SA283GRB properties, Material SA283GRB N, SA283GRB Material, SA283/SA283M, SA283GRB Steel, SA283GRB Yield, SA283GRB plate, SA283GRB HIC, SA283GRB NACE MR0175, SA283GRB ISO 15156, SA283GRB NACE MR0103, SA283GRB SSC

Keyword: SA283GRB,SA283GRB Steel Plate,SA283GRB Supplier

1.  SA283GRB Adopt standard: ASME SA283/SA283M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  SA283GRB Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA283GRB: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA283GRB Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Cu%(min) | Cu%(<=40mm) | Cu%(>40mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SA283GRB | 0.17 | 0.9 | 0.035 | 0.04 | 0.2 | 0.4 | 0.15-0.4 |

5.  SA283GRB Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA283GRB | 185 Mpa | 345-450Mpa | <=50MM | 28% |
|  | 185Mpa | 345-450Mpa | 50-200MM | 25% |

6.  Normally SA283/SA283M SA283GRB plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA283GRB Delivery Time Or Lead Time: 20-35days

8.  SA283GRB Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA283GRB, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA283/SA283M SA283GRB NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA283GRB,SA283/SA283M SA283GRB,SA283GRB Steel Plate,SA283GRB HIC,SA283GRB Nace

Tags: SA283GRB,SA283/SA283M SA283GRB,SA283GRB Steel Plate,SA283GRB steel factory, SA283GRB adopt standard, SA283GRB Heat treatment, SA283GRB Technical delivery condition, SA283GRB Chemical, SA283GRB Mechanical property, SA283GRB Price, SA283GRB CEV, SA283GRB Impact degree, SA283GRB impact energy, SA283GRB Supplier,SA283GRB Specification, SA283GRB properties, Material SA283GRB N, SA283GRB Material, SA283/SA283M, SA283GRB Steel, SA283GRB Yield, SA283GRB plate, SA283GRB HIC, SA283GRB NACE MR0175, SA283GRB ISO 15156, SA283GRB NACE MR0103, SA283GRB SSC