SA387GR21L,SA387GR21L Steel Plate,SA387GR21L Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA387/SA387M SA387GR21L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. SA387GR21L,SA387/SA387M SA387GR21L,SA387GR21L Steel Plate,SA387GR21L HIC,SA387GR21L Nace

Tags: SA387GR21L,SA387/SA387M SA387GR21L,SA387GR21L Steel Plate,SA387GR21L steel factory, SA387GR21L adopt standard, SA387GR21L Heat treatment, SA387GR21L Technical delivery condition, SA387GR21L Chemical, SA387GR21L Mechanical property, SA387GR21L Price, SA387GR21L CEV, SA387GR21L Impact degree, SA387GR21L impact energy, SA387GR21L Supplier,SA387GR21L Specification, SA387GR21L properties, Material SA387GR21L N, SA387GR21L Material, SA387/SA387M, SA387GR21L Steel, SA387GR21L Yield, SA387GR21L plate, SA387GR21L HIC, SA387GR21L NACE MR0175, SA387GR21L ISO 15156, SA387GR21L NACE MR0103, SA387GR21L SSC

Keyword: SA387GR21L,SA387GR21L Steel Plate,SA387GR21L Supplier

1.  SA387GR21L Adopt standard: ASME SA387/SA387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  SA387GR21L Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA387GR21L: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA387GR21L Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA387GR21L | 0.12 | 0.25-0.66 | 0.035 | 0.035 | 0.5 | 2.63-3.37 | 0.85-1.15 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  SA387GR21L Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA387GR21L | 205Mpa | 415-585Mpa | <=50MM | 18% |
|  | 205Mpa | 415-585Mpa | 50-200MM | -- |

6.  Normally SA387/SA387M SA387GR21L plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA387GR21L Delivery Time Or Lead Time: 20-35days

8.  SA387GR21L Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA387GR21L, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA387/SA387M SA387GR21L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA387GR21L,SA387/SA387M SA387GR21L,SA387GR21L Steel Plate,SA387GR21L HIC,SA387GR21L Nace

Tags: SA387GR21L,SA387/SA387M SA387GR21L,SA387GR21L Steel Plate,SA387GR21L steel factory, SA387GR21L adopt standard, SA387GR21L Heat treatment, SA387GR21L Technical delivery condition, SA387GR21L Chemical, SA387GR21L Mechanical property, SA387GR21L Price, SA387GR21L CEV, SA387GR21L Impact degree, SA387GR21L impact energy, SA387GR21L Supplier,SA387GR21L Specification, SA387GR21L properties, Material SA387GR21L N, SA387GR21L Material, SA387/SA387M, SA387GR21L Steel, SA387GR21L Yield, SA387GR21L plate, SA387GR21L HIC, SA387GR21L NACE MR0175, SA387GR21L ISO 15156, SA387GR21L NACE MR0103, SA387GR21L SSC