SA529 GRADE 55,SA529 GRADE 55 Steel Plate,SA529 GRADE 55 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA 529/SA 529M SA529 GRADE 55 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for High-Strength Carbon-Manganese Steel of Structural Quality Which is a large steel plate supplier mill at Gangsteel Group. SA529 GRADE 55,SA 529/SA 529M SA529 GRADE 55,SA529 GRADE 55 Steel Plate,SA529 GRADE 55 HIC,SA529 GRADE 55 Nace

Tags: SA529 GRADE 55,SA 529/SA 529M SA529 GRADE 55,SA529 GRADE 55 Steel Plate,SA529 GRADE 55 steel factory, SA529 GRADE 55 adopt standard, SA529 GRADE 55 Heat treatment, SA529 GRADE 55 Technical delivery condition, SA529 GRADE 55 Chemical, SA529 GRADE 55 Mechanical property, SA529 GRADE 55 Price, SA529 GRADE 55 CEV, SA529 GRADE 55 Impact degree, SA529 GRADE 55 impact energy, SA529 GRADE 55 Supplier,SA529 GRADE 55 Specification, SA529 GRADE 55 properties, Material SA529 GRADE 55 N, SA529 GRADE 55 Material, SA 529/SA 529M, SA529 GRADE 55 Steel, SA529 GRADE 55 Yield, SA529 GRADE 55 plate, SA529 GRADE 55 HIC, SA529 GRADE 55 NACE MR0175, SA529 GRADE 55 ISO 15156, SA529 GRADE 55 NACE MR0103, SA529 GRADE 55 SSC

Keyword: SA529 GRADE 55,SA529 GRADE 55 Steel Plate,SA529 GRADE 55 Supplier

1.  SA529 GRADE 55 Adopt standard: ASME SA 529/SA 529M Standard Specification for High-Strength Carbon-Manganese Steel of Structural Quality

2.  SA529 GRADE 55 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA529 GRADE 55: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA529 GRADE 55 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cu% |
| --- | --- | --- | --- | --- | --- | --- |
| SA529 GRADE 55 | 0.27 | 1.35 | 0.04 | 0.05 | 0.40 | 0.20 |

5.  SA529 GRADE 55 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA529 GRADE 55 | 380Mpa(min) | 485Mpa(min) | 200mm | -- |
|  | 380Mpa(min) | 690Mpa（max） | 50mm | -- |

6.  Normally SA 529/SA 529M SA529 GRADE 55 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA529 GRADE 55 Delivery Time Or Lead Time: 20-35days

8.  SA529 GRADE 55 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA529 GRADE 55, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA 529/SA 529M SA529 GRADE 55 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA529 GRADE 55,SA 529/SA 529M SA529 GRADE 55,SA529 GRADE 55 Steel Plate,SA529 GRADE 55 HIC,SA529 GRADE 55 Nace

Tags: SA529 GRADE 55,SA 529/SA 529M SA529 GRADE 55,SA529 GRADE 55 Steel Plate,SA529 GRADE 55 steel factory, SA529 GRADE 55 adopt standard, SA529 GRADE 55 Heat treatment, SA529 GRADE 55 Technical delivery condition, SA529 GRADE 55 Chemical, SA529 GRADE 55 Mechanical property, SA529 GRADE 55 Price, SA529 GRADE 55 CEV, SA529 GRADE 55 Impact degree, SA529 GRADE 55 impact energy, SA529 GRADE 55 Supplier,SA529 GRADE 55 Specification, SA529 GRADE 55 properties, Material SA529 GRADE 55 N, SA529 GRADE 55 Material, SA 529/SA 529M, SA529 GRADE 55 Steel, SA529 GRADE 55 Yield, SA529 GRADE 55 plate, SA529 GRADE 55 HIC, SA529 GRADE 55 NACE MR0175, SA529 GRADE 55 ISO 15156, SA529 GRADE 55 NACE MR0103, SA529 GRADE 55 SSC