SA533CL3,SA533CL3 Steel Plate,SA533CL3 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA533/SA533M SA533CL3 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for pressure Vessel Plates,Alloy Steel,Quenched and tempered,Manganese-Molybdenum and Manganese-Molybdenum-Nickel Which is a large steel plate supplier mill at Gangsteel Group. SA533CL3,SA533/SA533M SA533CL3,SA533CL3 Steel Plate,SA533CL3 HIC,SA533CL3 Nace

Tags: SA533CL3,SA533/SA533M SA533CL3,SA533CL3 Steel Plate,SA533CL3 steel factory, SA533CL3 adopt standard, SA533CL3 Heat treatment, SA533CL3 Technical delivery condition, SA533CL3 Chemical, SA533CL3 Mechanical property, SA533CL3 Price, SA533CL3 CEV, SA533CL3 Impact degree, SA533CL3 impact energy, SA533CL3 Supplier,SA533CL3 Specification, SA533CL3 properties, Material SA533CL3 N, SA533CL3 Material, SA533/SA533M, SA533CL3 Steel, SA533CL3 Yield, SA533CL3 plate, SA533CL3 HIC, SA533CL3 NACE MR0175, SA533CL3 ISO 15156, SA533CL3 NACE MR0103, SA533CL3 SSC

Keyword: SA533CL3,SA533CL3 Steel Plate,SA533CL3 Supplier

1.  SA533CL3 Adopt standard: ASME SA533/SA533MStandard Specification for pressure Vessel Plates,Alloy Steel,Quenched and tempered,Manganese-Molybdenum and Manganese-Molybdenum-Nickel

2.  SA533CL3 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA533CL3: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA533CL3 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SA533CL3 | 0.25 | 1.07-1.82 | 0.035 | 0.035 | 0.13-0.45 | 0.41-0.84 | 0.67-1.03 |

5.  SA533CL3 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA533CL3 | 570 Mpa | 690-860Mpa | <50MM | 16% |

6.  Normally SA533/SA533M SA533CL3 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA533CL3 Delivery Time Or Lead Time: 20-35days

8.  SA533CL3 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA533CL3, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA533/SA533MSA533CL3 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA533CL3,SA533/SA533M SA533CL3,SA533CL3 Steel Plate,SA533CL3 HIC,SA533CL3 Nace

Tags: SA533CL3,SA533/SA533M SA533CL3,SA533CL3 Steel Plate,SA533CL3 steel factory, SA533CL3 adopt standard, SA533CL3 Heat treatment, SA533CL3 Technical delivery condition, SA533CL3 Chemical, SA533CL3 Mechanical property, SA533CL3 Price, SA533CL3 CEV, SA533CL3 Impact degree, SA533CL3 impact energy, SA533CL3 Supplier,SA533CL3 Specification, SA533CL3 properties, Material SA533CL3 N, SA533CL3 Material, SA533/SA533M, SA533CL3 Steel, SA533CL3 Yield, SA533CL3 plate, SA533CL3 HIC, SA533CL3 NACE MR0175, SA533CL3 ISO 15156, SA533CL3 NACE MR0103, SA533CL3 SSC