JIS G 3103 SB410,SB410 Steel Plate,SB410 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB410 NACE MR0175, MR0103 Boiler steel plate, Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels Which is a large steel plate supplier mill at Gangsteel Group. SB410,JIS G 3103 SB410,SB410 Steel Plate,SB410 HIC,SB410 Nace

Tags: SB410,JIS G 3103 SB410,SB410 Steel Plate,SB410 steel factory, SB410 adopt standard, SB410 Heat treatment, SB410 Technical delivery condition, SB410 Chemical, SB410 Mechanical property, SB410 Price, SB410 CEV, SB410 Impact degree, SB410 impact energy, SB410 Supplier,SB410 Specification, SB410 properties, Material SB410 N, SB410 Material, JIS G 3103, SB410 Steel, SB410 Yield, SB410 plate, SB410 HIC, SB410 NACE MR0175, SB410 ISO 15156, SB410 NACE MR0103, SB410 SSC

Keyword: SB410,SB410 Steel Plate,SB410 Supplier

1.  SB410 Adopt standard: ASMT JIS G 3103 Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels

2.  SB410 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SB410: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SB410 Chemical composition % of the Product analysis of grade

| Grade | C %(<25mm) | C %(25-50mm) | C%(50-100mm) | C%(>100mm) | Si% | Mn% |
| --- | --- | --- | --- | --- | --- | --- |
| SB410 | 0.24 | 0.27 | 0.29 | 0.30 | 0.15-0.40 | 0.9 |
|  | P% | S% | Mo% |  |  |  |
|  | 0.030 | 0.03 | -- |  |  |  |

5.  SB410 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SB410 | 225Mpa(min) | 410-550Mpa | <25mm | 21% |
|  | 225Mpa(min) | 410-550Mpa | 25-50mm | 21% |
|  | 225Mpa(min) | 410-550Mpa | 50-100mm | 25% |
|  | 225Mpa(min) | 410-550Mpa | >100mm | 25% |

6.  Normally JIS G 3103 SB410 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SB410 Delivery Time Or Lead Time: 20-35days

8.  SB410 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SB410, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB410 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SB410,JIS G 3103 SB410,SB410 Steel Plate,SB410 HIC,SB410 Nace

Tags: SB410,JIS G 3103 SB410,SB410 Steel Plate,SB410 steel factory, SB410 adopt standard, SB410 Heat treatment, SB410 Technical delivery condition, SB410 Chemical, SB410 Mechanical property, SB410 Price, SB410 CEV, SB410 Impact degree, SB410 impact energy, SB410 Supplier,SB410 Specification, SB410 properties, Material SB410 N, SB410 Material, JIS G 3103, SB410 Steel, SB410 Yield, SB410 plate, SB410 HIC, SB410 NACE MR0175, SB410 ISO 15156, SB410 NACE MR0103, SB410 SSC