JIS G 3103 SB450,SB450 Steel Plate,SB450 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB450 NACE MR0175, MR0103 Boiler steel plate, Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels Which is a large steel plate supplier mill at Gangsteel Group. SB450,JIS G 3103 SB450,SB450 Steel Plate,SB450 HIC,SB450 Nace

Tags: SB450,JIS G 3103 SB450,SB450 Steel Plate,SB450 steel factory, SB450 adopt standard, SB450 Heat treatment, SB450 Technical delivery condition, SB450 Chemical, SB450 Mechanical property, SB450 Price, SB450 CEV, SB450 Impact degree, SB450 impact energy, SB450 Supplier,SB450 Specification, SB450 properties, Material SB450 N, SB450 Material, JIS G 3103, SB450 Steel, SB450 Yield, SB450 plate, SB450 HIC, SB450 NACE MR0175, SB450 ISO 15156, SB450 NACE MR0103, SB450 SSC

Keyword: SB450,SB450 Steel Plate,SB450 Supplier

1.  SB450 Adopt standard: ASMT JIS G 3103 Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels

2.  SB450 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SB450: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SB450 Chemical composition % of the Product analysis of grade

| Grade | C %(<25mm) | C %(25-50mm) | C%(>50mm) | Si% | Mn% | P% |
| --- | --- | --- | --- | --- | --- | --- |
| SB450 | 0.28 | 0.31 | 0.33 | 0.15-0.4 | 0.9 | 0.03 |
|  | S% | Mo% |  |  |  |  |
|  | 0.03 | -- |  |  |  |  |

5.  SB450 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SB450 | 245Mpa(min) | 450-590Mpa | <25mm | 19% |
|  | 245Mpa(min) | 450-590Mpa | 25-50mm | 19% |
|  | 245Mpa(min) | 450-590Mpa | 50-100mm | 23% |

6.  Normally JIS G 3103 SB450 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SB450 Delivery Time Or Lead Time: 20-35days

8.  SB450 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SB450, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB450 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SB450,JIS G 3103 SB450,SB450 Steel Plate,SB450 HIC,SB450 Nace

Tags: SB450,JIS G 3103 SB450,SB450 Steel Plate,SB450 steel factory, SB450 adopt standard, SB450 Heat treatment, SB450 Technical delivery condition, SB450 Chemical, SB450 Mechanical property, SB450 Price, SB450 CEV, SB450 Impact degree, SB450 impact energy, SB450 Supplier,SB450 Specification, SB450 properties, Material SB450 N, SB450 Material, JIS G 3103, SB450 Steel, SB450 Yield, SB450 plate, SB450 HIC, SB450 NACE MR0175, SB450 ISO 15156, SB450 NACE MR0103, SB450 SSC