JIS G 3103 SB450M,SB450M Steel Plate,SB450M Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB450M NACE MR0175, MR0103 Boiler steel plate, Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels Which is a large steel plate supplier mill at Gangsteel Group. SB450M,JIS G 3103 SB450M,SB450M Steel Plate,SB450M HIC,SB450M Nace

Tags: SB450M,JIS G 3103 SB450M,SB450M Steel Plate,SB450M steel factory, SB450M adopt standard, SB450M Heat treatment, SB450M Technical delivery condition, SB450M Chemical, SB450M Mechanical property, SB450M Price, SB450M CEV, SB450M Impact degree, SB450M impact energy, SB450M Supplier,SB450M Specification, SB450M properties, Material SB450M N, SB450M Material, JIS G 3103, SB450M Steel, SB450M Yield, SB450M plate, SB450M HIC, SB450M NACE MR0175, SB450M ISO 15156, SB450M NACE MR0103, SB450M SSC

Keyword: SB450M,SB450M Steel Plate,SB450M Supplier

1.  SB450M Adopt standard: ASMT JIS G 3103 Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels

2.  SB450M Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SB450M: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SB450M Chemical composition % of the Product analysis of grade

| Grade | C %(<25mm) | C %(25-50mm) | C%(50-100mm) | C%(>100mm) | Si% | Mn% |
| --- | --- | --- | --- | --- | --- | --- |
| SB450M | 0.18 | 0.21 | 0.23 | 0.25 | 0.15-0.4 | 0.9 |
|  | P% | S% | Mo% |  |  |  |
|  | 0.03 | 0.03 | 0.45-0.6 |  |  |  |

5.  SB450M Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SB450M | 255Mpa(min) | 450-590Mpa | <25mm | 19% |
|  | 255Mpa(min) | 450-590Mpa | 25-100mm | 19% |
|  | 255Mpa(min) | 450-590Mpa | >100mm | 23% |

6.  Normally JIS G 3103 SB450M plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SB450M Delivery Time Or Lead Time: 20-35days

8.  SB450M Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SB450M, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB450M NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SB450M,JIS G 3103 SB450M,SB450M Steel Plate,SB450M HIC,SB450M Nace

Tags: SB450M,JIS G 3103 SB450M,SB450M Steel Plate,SB450M steel factory, SB450M adopt standard, SB450M Heat treatment, SB450M Technical delivery condition, SB450M Chemical, SB450M Mechanical property, SB450M Price, SB450M CEV, SB450M Impact degree, SB450M impact energy, SB450M Supplier,SB450M Specification, SB450M properties, Material SB450M N, SB450M Material, JIS G 3103, SB450M Steel, SB450M Yield, SB450M plate, SB450M HIC, SB450M NACE MR0175, SB450M ISO 15156, SB450M NACE MR0103, SB450M SSC