JIS G3115 SPV315,SPV315 Steel Plate,SPV315 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G3115 SPV315 NACE MR0175, MR0103 Boiler steel plate, Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels Which is a large steel plate supplier mill at Gangsteel Group. SPV315,JIS G3115 SPV315,SPV315 Steel Plate,SPV315 HIC,SPV315 Nace

Tags: SPV315,JIS G3115 SPV315,SPV315 Steel Plate,SPV315 steel factory, SPV315 adopt standard, SPV315 Heat treatment, SPV315 Technical delivery condition, SPV315 Chemical, SPV315 Mechanical property, SPV315 Price, SPV315 CEV, SPV315 Impact degree, SPV315 impact energy, SPV315 Supplier,SPV315 Specification, SPV315 properties, Material SPV315 N, SPV315 Material, JIS G3115, SPV315 Steel, SPV315 Yield, SPV315 plate, SPV315 HIC, SPV315 NACE MR0175, SPV315 ISO 15156, SPV315 NACE MR0103, SPV315 SSC

Keyword: SPV315,SPV315 Steel Plate,SPV315 Supplier

1.  SPV315 Adopt standard: ASMT JIS G3115 Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels

2.  SPV315 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SPV315: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SPV315 Chemical composition % of the Product analysis of grade

| Grade | C %(<100mm) | Si% | Mn% | P% | S% |  |
| --- | --- | --- | --- | --- | --- | --- |
| SPV315 | 0.18 | 0.55 | 1.6 | 0.03 | 0.03 |  |

5.  SPV315 Mechanical Property

| Grade | Thicknesss | Min Yield | Tensile | Elongation |
| --- | --- | --- | --- | --- |
|  |  |  |  | Thicknesss |  |
| SPV315 | 6-50mm | 315Mpa(min) | 490-610Mpa | <=16mm | 16% |
|  | 50-100mm | 295Mpa(min) | 490-610Mpa | >16mm | 20% |
|  | 100-200mm | 275Mpa(min) | 490-610Mpa | >40mm | 23% |

6.  Normally JIS G3115 SPV315 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SPV315 Delivery Time Or Lead Time: 20-35days

8.  SPV315 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SPV315, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G3115 SPV315 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SPV315,JIS G3115 SPV315,SPV315 Steel Plate,SPV315 HIC,SPV315 Nace

Tags: SPV315,JIS G3115 SPV315,SPV315 Steel Plate,SPV315 steel factory, SPV315 adopt standard, SPV315 Heat treatment, SPV315 Technical delivery condition, SPV315 Chemical, SPV315 Mechanical property, SPV315 Price, SPV315 CEV, SPV315 Impact degree, SPV315 impact energy, SPV315 Supplier,SPV315 Specification, SPV315 properties, Material SPV315 N, SPV315 Material, JIS G3115, SPV315 Steel, SPV315 Yield, SPV315 plate, SPV315 HIC, SPV315 NACE MR0175, SPV315 ISO 15156, SPV315 NACE MR0103, SPV315 SSC