JIS G3115 SPV450,SPV450 Steel Plate,SPV450 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G3115 SPV450 NACE MR0175, MR0103 Boiler steel plate, Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels Which is a large steel plate supplier mill at Gangsteel Group. SPV450,JIS G3115 SPV450,SPV450 Steel Plate,SPV450 HIC,SPV450 Nace

Tags: SPV450,JIS G3115 SPV450,SPV450 Steel Plate,SPV450 steel factory, SPV450 adopt standard, SPV450 Heat treatment, SPV450 Technical delivery condition, SPV450 Chemical, SPV450 Mechanical property, SPV450 Price, SPV450 CEV, SPV450 Impact degree, SPV450 impact energy, SPV450 Supplier,SPV450 Specification, SPV450 properties, Material SPV450 N, SPV450 Material, JIS G3115, SPV450 Steel, SPV450 Yield, SPV450 plate, SPV450 HIC, SPV450 NACE MR0175, SPV450 ISO 15156, SPV450 NACE MR0103, SPV450 SSC

Keyword: SPV450,SPV450 Steel Plate,SPV450 Supplier

1.  SPV450 Adopt standard: ASMT JIS G3115 Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels

2.  SPV450 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SPV450: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SPV450 Chemical composition % of the Product analysis of grade

| Grade | C % | Si% | Mn% | P% | S% |  |
| --- | --- | --- | --- | --- | --- | --- |
| SPV450 | 0.18 | 0.75 | 1.6 | 0.03 | 0.03 |  |

5.  SPV450 Mechanical Property

| Grade | Thicknesss | Min Yield | Tensile | Elongation |
| --- | --- | --- | --- | --- |
|  |  |  |  | Thicknesss |  |
| SPV450 | 6-50mm | 450Mpa(min) | 570-700Mpa | <=16mm | 19% |
|  | 50-100mm | 430Mpa(min) | 570-700Mpa | >16mm | 26% |
|  | 100-200mm | 410Mpa(min) | 570-700Mpa | >40mm | 20% |

6.  Normally JIS G3115 SPV450 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SPV450 Delivery Time Or Lead Time: 20-35days

8.  SPV450 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SPV450, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G3115 SPV450 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SPV450,JIS G3115 SPV450,SPV450 Steel Plate,SPV450 HIC,SPV450 Nace

Tags: SPV450,JIS G3115 SPV450,SPV450 Steel Plate,SPV450 steel factory, SPV450 adopt standard, SPV450 Heat treatment, SPV450 Technical delivery condition, SPV450 Chemical, SPV450 Mechanical property, SPV450 Price, SPV450 CEV, SPV450 Impact degree, SPV450 impact energy, SPV450 Supplier,SPV450 Specification, SPV450 properties, Material SPV450 N, SPV450 Material, JIS G3115, SPV450 Steel, SPV450 Yield, SPV450 plate, SPV450 HIC, SPV450 NACE MR0175, SPV450 ISO 15156, SPV450 NACE MR0103, SPV450 SSC