SA710CL2,SA710CL2 Steel Plate,SA710CL2 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710M SA710CL2 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates, Which is a large steel plate supplier mill at Gangsteel Group. SA710CL2,SA710/SA710M SA710CL2,SA710CL2 Steel Plate,SA710CL2 HIC,SA710CL2 Nace

Tags: SA710CL2,SA710/SA710M SA710CL2,SA710CL2 Steel Plate,SA710CL2 steel factory, SA710CL2 adopt standard, SA710CL2 Heat treatment, SA710CL2 Technical delivery condition, SA710CL2 Chemical, SA710CL2 Mechanical property, SA710CL2 Price, SA710CL2 CEV, SA710CL2 Impact degree, SA710CL2 impact energy, SA710CL2 Supplier,SA710CL2 Specification, SA710CL2 properties, Material SA710CL2 N, SA710CL2 Material, A710/A710M, SA710CL2 Steel, SA710CL2 Yield, SA710CL2 plate, SA710CL2 HIC, SA710CL2 NACE MR0175, SA710CL2 ISO 15156, SA710CL2 NACE MR0103, SA710CL2 SSC

Keyword: SA710CL2,SA710CL2 Steel Plate,SA710CL2 Supplier

1.  SA710CL2 Adopt standard: ASME SA710/SA710M Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates.

2.  SA710CL2 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA710CL2: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA710CL2 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Ni% |
| --- | --- | --- | --- | --- | --- | --- |
| SA710CL2 | 0.07 | 0.40-0.70 | 0.025 | 0.025 | 0.4 | 0.7-1.0 |
|  | Mo% | Cu% | Cb% | Ti% | Cr% |  |
|  | 0.15-0.25 | 1.0-1.3 | 0.02 | -- | 0.6-0.9 |  |

5.  SA710CL2 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA710CL2 | 450Mpa | 495Mpa | <6.5mm | 20% |
|  | 450Mpa | 495Mpa | 6.5-8mm | 20% |
|  | 450Mpa | 495Mpa | 8-10mm | 20% |
|  | 450Mpa | 495Mpa | 10-12.5mm | 20% |
|  | 450Mpa | 495Mpa | 12.5-20mm | 20% |
|  | 450 Mpa | 495Mpa | 20-25mm | 20% |
|  | 415 Mpa | 495Mpa | 25-30mm | 20% |
|  | 415 Mpa | 495Mpa | 30-50mm | 20% |
|  | 380Mpa | 450Mpa | 50-100mm | -- |
|  | 345Mpa | 415Mpa | >100mm | -- |

6.  Normally SA710/SA710M SA710CL2 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA710CL2 Delivery Time Or Lead Time: 20-35days

8.  SA710CL2 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA710CL2, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A710/A710MSA710CL2 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA710CL2,SA710/SA710M SA710CL2,SA710CL2 Steel Plate,SA710CL2 HIC,SA710CL2 Nace

Tags: SA710CL2,SA710/SA710M SA710CL2,SA710CL2 Steel Plate,SA710CL2 steel factory, SA710CL2 adopt standard, SA710CL2 Heat treatment, SA710CL2 Technical delivery condition, SA710CL2 Chemical, SA710CL2 Mechanical property, SA710CL2 Price, SA710CL2 CEV, SA710CL2 Impact degree, SA710CL2 impact energy, SA710CL2 Supplier,SA710CL2 Specification, SA710CL2 properties, Material SA710CL2 N, SA710CL2 Material, A710/A710M, SA710CL2 Steel, SA710CL2 Yield, SA710CL2 plate, SA710CL2 HIC, SA710CL2 NACE MR0175, SA710CL2 ISO 15156, SA710CL2 NACE MR0103, SA710CL2 SSC