SA738GRA,SA738GRA Steel Plate,SA738GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M SA738GRA NACE MR0175, MR0103 Boiler steel plate, Specification for pressure plates,heat-treated,carbon-manganese-silicon steel ,for moderate and lower temperature service. Which is a large steel plate supplier mill at Gangsteel Group. SA738GRA,SA-738/SA-738M SA738GRA,SA738GRA Steel Plate,SA738GRA HIC,SA738GRA Nace

Tags: SA738GRA,SA-738/SA-738M SA738GRA,SA738GRA Steel Plate,SA738GRA steel factory, SA738GRA adopt standard, SA738GRA Heat treatment, SA738GRA Technical delivery condition, SA738GRA Chemical, SA738GRA Mechanical property, SA738GRA Price, SA738GRA CEV, SA738GRA Impact degree, SA738GRA impact energy, SA738GRA Supplier,SA738GRA Specification, SA738GRA properties, Material SA738GRA N, SA738GRA Material, SA-738/SA-738M, SA738GRA Steel, SA738GRA Yield, SA738GRA plate, SA738GRA HIC, SA738GRA NACE MR0175, SA738GRA ISO 15156, SA738GRA NACE MR0103, SA738GRA SSC

Keyword: SA738GRA,SA738GRA Steel Plate,SA738GRA Supplier

1.  SA738GRA Adopt standard: ASME SA-738/SA-738M Specification for pressure plates,heat-treated,carbon-manganese-silicon steel.

2.  SA738GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA738GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA738GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<65mm) | Mn %(>65mm) | P% | S% | Si% | Cu% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA738GRA | 0.24 | 1.62 | 1.72 | 0.035 | 0.035 | 0.13-0.55 | 0.38 | 0.53 |
|  | Cr% | Mo%(40mm) | Mo%(<40mm) | V% | Cb% | Cb plus V |  |  |
|  | 0.29 | 0.08 | 0.08 | 0.08 | 0.05 | 0.10 |  |  |

5.  SA738GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA738GRA | 310 Mpa | 515-655Mpa | <65MM | 20% |
|  | 310 Mpa | 515-655Mpa | 65-100MM | 20% |
|  | 310 Mpa | 515-655Mpa | >100MM | 20% |

6.  Normally SA-738/SA-738M SA738GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA738GRA Delivery Time Or Lead Time: 20-35days

8.  SA738GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA738GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M SA738GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA738GRA,SA-738/SA-738M SA738GRA,SA738GRA Steel Plate,SA738GRA HIC,SA738GRA Nace

Tags: SA738GRA,SA-738/SA-738M SA738GRA,SA738GRA Steel Plate,SA738GRA steel factory, SA738GRA adopt standard, SA738GRA Heat treatment, SA738GRA Technical delivery condition, SA738GRA Chemical, SA738GRA Mechanical property, SA738GRA Price, SA738GRA CEV, SA738GRA Impact degree, SA738GRA impact energy, SA738GRA Supplier,SA738GRA Specification, SA738GRA properties, Material SA738GRA N, SA738GRA Material, SA-738/SA-738M, SA738GRA Steel, SA738GRA Yield, SA738GRA plate, SA738GRA HIC, SA738GRA NACE MR0175, SA738GRA ISO 15156, SA738GRA NACE MR0103, SA738GRA SSC