SA738GRB,SA738GRB Steel Plate,SA738GRB Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M SA738GRB NACE MR0175, MR0103 Boiler steel plate, Specification for pressure plates,heat-treated,carbon-manganese-silicon steel ,for moderate and lower temperature service. Which is a large steel plate supplier mill at Gangsteel Group. SA738GRB,SA-738/SA-738M SA738GRB,SA738GRB Steel Plate,SA738GRB HIC,SA738GRB Nace

Tags: SA738GRB,SA-738/SA-738M SA738GRB,SA738GRB Steel Plate,SA738GRB steel factory, SA738GRB adopt standard, SA738GRB Heat treatment, SA738GRB Technical delivery condition, SA738GRB Chemical, SA738GRB Mechanical property, SA738GRB Price, SA738GRB CEV, SA738GRB Impact degree, SA738GRB impact energy, SA738GRB Supplier,SA738GRB Specification, SA738GRB properties, Material SA738GRB N, SA738GRB Material, SA-738/SA-738M, SA738GRB Steel, SA738GRB Yield, SA738GRB plate, SA738GRB HIC, SA738GRB NACE MR0175, SA738GRB ISO 15156, SA738GRB NACE MR0103, SA738GRB SSC

Keyword: SA738GRB,SA738GRB Steel Plate,SA738GRB Supplier

1.  SA738GRB Adopt standard: ASME SA-738/SA-738M Specification for pressure plates,heat-treated,carbon-manganese-silicon steel.

2.  SA738GRB Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA738GRB: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA738GRB Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<65mm) | Mn %(>65mm) | P% | S% | Si% | Cu% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA738GRB | 0.20 | 0.84-1.62 | 0.84-1.72 | 0.030 | 0.030 | 0.13-0.60 | 0.38 | 0.63 |
|  | Cr% | Mo%(40mm) | Mo%(<40mm) | V% | Cb% | Cb plus V |  |  |
|  | 0.34 | 0.30 | 0.33 | 0.08 | 0.05 | 0.10 |  |  |

5.  SA738GRB Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA738GRB | 415 Mpa | 585-705Mpa | <65MM | 20% |
|  | 415 Mpa | 585-705Mpa | 65-100MM | 20% |
|  | 415 Mpa | 585-705Mpa | >100MM | 20% |

6.  Normally SA-738/SA-738M SA738GRB plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA738GRB Delivery Time Or Lead Time: 20-35days

8.  SA738GRB Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA738GRB, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M SA738GRB NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA738GRB,SA-738/SA-738M SA738GRB,SA738GRB Steel Plate,SA738GRB HIC,SA738GRB Nace

Tags: SA738GRB,SA-738/SA-738M SA738GRB,SA738GRB Steel Plate,SA738GRB steel factory, SA738GRB adopt standard, SA738GRB Heat treatment, SA738GRB Technical delivery condition, SA738GRB Chemical, SA738GRB Mechanical property, SA738GRB Price, SA738GRB CEV, SA738GRB Impact degree, SA738GRB impact energy, SA738GRB Supplier,SA738GRB Specification, SA738GRB properties, Material SA738GRB N, SA738GRB Material, SA-738/SA-738M, SA738GRB Steel, SA738GRB Yield, SA738GRB plate, SA738GRB HIC, SA738GRB NACE MR0175, SA738GRB ISO 15156, SA738GRB NACE MR0103, SA738GRB SSC