SA738GRC,SA738GRC Steel Plate,SA738GRC Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M SA738GRC NACE MR0175, MR0103 Boiler steel plate, Specification for pressure plates,heat-treated,carbon-manganese-silicon steel ,for moderate and lower temperature service. Which is a large steel plate supplier mill at Gangsteel Group. SA738GRC,SA-738/SA-738M SA738GRC,SA738GRC Steel Plate,SA738GRC HIC,SA738GRC Nace

Tags: SA738GRC,SA-738/SA-738M SA738GRC,SA738GRC Steel Plate,SA738GRC steel factory, SA738GRC adopt standard, SA738GRC Heat treatment, SA738GRC Technical delivery condition, SA738GRC Chemical, SA738GRC Mechanical property, SA738GRC Price, SA738GRC CEV, SA738GRC Impact degree, SA738GRC impact energy, SA738GRC Supplier,SA738GRC Specification, SA738GRC properties, Material SA738GRC N, SA738GRC Material, SA-738/SA-738M, SA738GRC Steel, SA738GRC Yield, SA738GRC plate, SA738GRC HIC, SA738GRC NACE MR0175, SA738GRC ISO 15156, SA738GRC NACE MR0103, SA738GRC SSC

Keyword: SA738GRC,SA738GRC Steel Plate,SA738GRC Supplier

1.  SA738GRC Adopt standard: ASME SA-738/SA-738M Specification for pressure plates,heat-treated,carbon-manganese-silicon steel.

2.  SA738GRC Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA738GRC: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA738GRC Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<65mm) | Mn %(>65mm) | P% | S% | Si% | Cu% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA738GRC | 0.24 | 1.62 | 1.72 | 0.025 | 0.025 | 0.13-0.55 | 0.38 | 0.53 |
|  | Cr% | Mo%(40mm) | Mo%(<40mm) | V% | Cb% | Cb plus V |  |  |
|  | 0.29 | 0.08 | 0.08 | 0.05 | -- | -- |  |  |

5.  SA738GRC Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA738GRC | 415 Mpa | 550-690Mpa | <65MM | 22% |
|  | 380 Mpa | 515-655Mpa | 65-100MM | 22% |
|  | 315 Mpa | 485-655Mpa | >100MM | 20% |

6.  Normally SA-738/SA-738M SA738GRC plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA738GRC Delivery Time Or Lead Time: 20-35days

8.  SA738GRC Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA738GRC, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M SA738GRC NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA738GRC,SA-738/SA-738M SA738GRC,SA738GRC Steel Plate,SA738GRC HIC,SA738GRC Nace

Tags: SA738GRC,SA-738/SA-738M SA738GRC,SA738GRC Steel Plate,SA738GRC steel factory, SA738GRC adopt standard, SA738GRC Heat treatment, SA738GRC Technical delivery condition, SA738GRC Chemical, SA738GRC Mechanical property, SA738GRC Price, SA738GRC CEV, SA738GRC Impact degree, SA738GRC impact energy, SA738GRC Supplier,SA738GRC Specification, SA738GRC properties, Material SA738GRC N, SA738GRC Material, SA-738/SA-738M, SA738GRC Steel, SA738GRC Yield, SA738GRC plate, SA738GRC HIC, SA738GRC NACE MR0175, SA738GRC ISO 15156, SA738GRC NACE MR0103, SA738GRC SSC