A 572 Grade 60 Steel plates,A572Gr60 Steel Supplier

1. A572 steel plate is used in a variety of structural applications including bridges, buildings, construction equipment, freight cars, machinery, truck parts and transmission towers.

2. A572 steel plate is produced in five grades: 42, 50, 55, 60 and 65.

3. High Strength Low Alloy (HSLA) Steel Plate

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| High Strength Low Alloy (HSLA) Steel Plate | | | | |
| all measurement in Inches | | Thickness | Width | Length |
| A572 | Grade 42 | Over 4" – 6" | 48" – 120" | 96" – 480" |
| Grade 50 | 3/16" – 4" | 48" – 120" | 96" – 480" |
| Grade 55 | 3/16" – 1-1/2" | 48" – 120" | 96" – 480" |
| Grade 60 | 3/16" – 1-1/4" | 48" – 120" | 96" – 480" |
| Grade 65 | 3/16" – 1-1/4" | 48" – 120" | 96" – 650" |

4.Other steel plate grade

A 36 A572 Grade 42, 50, 60, 65

C SA G40.21 Gr 44W, 50W, 50A A709 Gr 36, 50, 50W

A709 Gr HPS 50W, 70W A ASHTO M270 Gr50, 50W

A588 & A606 A871-65

A656 Gr 50, 60, 70, 80 A573 Gr 58, 65, 70

A283

5. If you have any other requirement for steel plate, please feel free to contact us.