AR500,AR500F Steel Plate Supplier

1. AR500F steel plate is a premium abrasion resistant steel plate, heat treated to exhibit through-hardening, improved forming and welding capabilities. With a typical BHN of 460 – 544, the protection AR500F provides in wear applications is exceptional. Used in the manufacture of mining equipment, the truck-trailer industry and the concrete / aggregate industry, AR500F steel possesses excellent resistance to slide wear, rub wear and heavy wear. It can also withstand high impact stresses, even at extremely low temperatures.

2. Each producing mill has its own proprietary chemical composition and heat-treating process for AR 500F.

|  |  |  |  |
| --- | --- | --- | --- |
| Abrasion Resistant Steel Plate | | | |
| all measurement in Inches | Thickness | Width | Length |
| AR500 | 3/16" – 2" | 48" – 96" | 96" – 480" |

3. If you have any other requirement for steel plate, please feel free to contact us.