EN1522, MIL-A 46100D Armour Plate

UNITEDSTEEL supplies a comprehensive range of Miilux Protection steels from 380 to 500 Brinell in thicknesses from 2.5 mm to 40 mm. Plates are ballistic tested meeting the standards of most international authorities including EN1522, MIL-A 46100D, and STANAG 4569. Stocks of Miilux Protection are held in our warehouses and distribution facilities.

About Miilux Protection

Miilux Protection is an established brand of protection steel with a global reputation for high quality and integrity. We can supply this specialist steel to the specifications below:

Specifications/Grades

Miilux Protection 380
Hardness 320 - 370HB
Supplied from 6mm to 25mm thick

Miilux Protection 400
Hardness 360 - 420HB
Supplied from 5mm to 40mm thick

Miilux Protection 450
Hardness 420 – 480HB
Supplied from 5mm to 40mm thick

Miilux Protection 500
Hardness 480 – 540HB
Supplied from 2.5mm to 40mm thick

Miilux Protection 500T
Hardness 480 – 540HB
Supplied from 2.5mm to 40mm thick

Plate formats for all grades of Miilux Protection are available up to 6100 x 2500 mm

If you have any other requirement for steel plate, please feel free to contact us.